## Slide 1: First-Principle Calculations of Oxide Perovskite Semiconductors
David-Alexander Robinson Sch.
Dr. Anderson Janotti
Prof. Chris Van de Walle
Computational Materials Group
Materials Research Laboratory, UCSB

## Slide 2: Introduction
Complex Oxide Perovskite Semiconductors; Crystals of the form ABO3
  A = Mono-, Di- or Trivalent element; Li, K, Mg, Ca, Sr, Ba, Sc, Y, La, Gd
  B = Transition Metal cation; Ti, Zr, Hf, Y, Nb, Ta or; Al, Ga, In
Implications?
  Explaining experimental results using fundamental theory.
  Novel electronic materials.
    Transparent conductors; Wide Band-Gap Semiconductors.

## Slide 3: Methods
Hybrid Functionals
  Heyd-Scuseria-Ernzerhof (HSE)
  Combines both Hartree-Fock and Density Functional Theory methods to give a more accurate result.
Vienna Ab-initio Simulation Package (VASP) code
  An Iterative method.
  VASP works to minimise the energy of the system by filling up electron bands and relaxing the lattice constant in turn
High Performance Computing
  California NanoSystems Institute (CNSI), UCSB.
  Ranger Cluster, Texas Advanced Computing Center, U Texas.

## Slide 4: Results I
a = 0.395 nm
a = 0.414 nm
a = 0.419 nm
SrTiO3
SrHfO3
SrZrO3
Band Structure Plot
Comparisons using GGA (General Gradient Approximation)

## Slide 5: Results II
a = 0.395 nm
a = 0.414 nm
a = 0.419 nm
SrTiO3
SrHfO3
SrZrO3
Band Structure Plot
Comparisons using HSE
(Heyd-Scuseria-Ernzerhof )

## Slide 6: Results III
a = 0.39483 nm; Eg = 1.8 eV
SrTiO3 using GGA
HSE vs. GGA
  Accepted experimental values
  a = 0.3905 nm; Eg = 3.25 eV
a = 0.39046 nm ; Eg = 3.332 eV
SrTiO3 using HSE

## Slide 7: Results IV
Lattice Constants and Indirect R-Γ band gaps, using GGA and HSE
    On using HSE we get band gap widening of 1.5±0.2 eV *
crystal | a (nm) [GGA] | a (nm) [HSE] | Eg (eV) [GGA] | Eg (eV) [HSE] | Eg diff (eV)
BaTiO_3 | 0.40380 | 0.39934 | 1.5436 | 3.1847 | 1.6411
BaZrO_3 | 0.42506 | 0.42276 | 2.9927 | 4.5073 | 1.5146
CaTiO_3 | 0.38964 | 0.38511 | 1.7036 | 3.4088 | 1.7051
GdAlO_3 | 0.37256 | 0.36835 | 2.9004 | 4.3289 | 1.4285
GdGaO_3 | 0.38431 | 0.3796 | 2.8069 | 4.2252 | 1.4183
LaAlO_3 | 0.38098 | 0.37772 | 3.4934 | 4.8867 | 1.3933
LaGaO_3 | 0.39280 | 0.38738 | 3.3386 | 4.7459 | 1.4072
MgTiO_3 | 0.38510 | 0.38004 | 1.6005 | 3.1846 | 1.5841
ScAlO_3 | 0.36457 | 0.36063 | 2.2320 | 2.8631 | 0.6311
SrTiO_3 | 0.39483 | 0.39046 | 1.6465 | 3.3326 | 1.6861
SrZrO_3 | 0.41943 | 0.39049 | 3.1819 | 3.3171 | 0.1352
Y.AlO_3 | 0.37182 | 0.36814 | 2.8012 | 2.7757 | -0.0255

## Slide 8: Results V
Electrostatic Potential, V
Band Alignment Calculations;
  Gives a Valance Band Offset of 0.19 eV
Displacement, x
LaAlO3-GdAlO3

## Slide 9: Results VI
Electrostatic Potential, V
Band Alignment Calculations;
  Gives a Valance Band Offset of 0.44 eV
Displacement, x
LaAlO3-GdAlO3