## Slide 1: First-Principle Calculations of Oxide Perovskite Semiconductors
David-Alexander Robinson Sch., Trinity College Dublin
Dr. Anderson Janotti
Prof. Chris Van de Walle
Computational Materials Group
Materials Research Laboratory, UCSB

## Slide 2: Introduction
Complex Oxide Perovskite Semiconductors; Crystals of the form ABO3
  A = Mono-, Di- or Trivalent element; Li, K, Mg, Ca, Sr, Ba, Sc, Y, La, Gd
  B = Transition Metal cation; Ti, Zr, Hf, Y, Nb, Ta or; Al, Ga, In
Implications?
  Explaining experimental results using fundamental theory.
  Novel electronic materials.
    Transparent conductors; Wide Band-Gap Semiconductors.
SrTiO3
Valence band
maximum

## Slide 3: Methods
We wish to solve the many-electron quantum mechanical equations for the electronic structure of solids.
Hartree-Fock (HF)
  The many-electron wavefuntion is written as an anti-symmetric linear combination of single electron wavefunctions.
Density Functional Theory (DFT)
  Replaces the many-electron problem with a single-particle in an effective potential.
  1998 Nobel Prize awarded to Walter Kohn for his work on DFT.
Hybrid Functionals
  Heyd-Scuseria-Ernzerhof (HSE)
  Mixes both HF and DFT exchange potential to give a more accurate description of the electronic structure.

## Slide 4: Methods
Vienna Ab-initio Simulation Package (VASP) code
  A self-consistent iterative method which works to minimise the energy of the system by filling up electron bands and relaxing the lattice constant in turn
  Solves the quantum mechanical Schrödinger equation.
  The calculation uses First Principle methods and so no empirical input parameters are needed.
High Performance Computing
  California NanoSystems Institute (CNSI), UCSB.
  Lattice, Guild and Knot clusters.
  Lonestar Cluster, Texas Advanced Computing Center, U Texas.
Computer Programming
  Linux, bash, VI, XMGrace

## Slide 5: Results I
a = 0.3948 nm ; Eg = 1.65 eV
a = 0.4142 nm ; Eg = 3.70 eV
a = 0.4194 nm ; Eg = 3.18 eV
SrTiO3
SrHfO3
SrZrO3
Band Structure Plot
Comparisons using GGA (General Gradient Approximation)

## Slide 6: Results II
a = 0.3905 nm ; Eg = 3.33 eV
a = 0.4109 nm ; Eg = 5.30 eV
a = 0.4142 nm ; Eg = 4.88 eV
SrTiO3
SrHfO3
SrZrO3
Band Structure Plot
Comparisons using HSE
(Heyd-Scuseria-Ernzerhof )

## Slide 7: Results III
a = 0.3948 nm; Eg = 1.65 eV
SrTiO3 using GGA
HSE vs. GGA
  Accepted experimental values
  a = 0.3905 nm; Eg = 3.25 eV
a = 0.3905 nm ; Eg = 3.33 eV
SrTiO3 using HSE

## Slide 8: Results IV
Lattice Constants and Indirect R-Γ band gaps, using GGA and HSE
    On using HSE we get band gap widening of 1.54 ± 0.16 eV
Crystal | a (nm) [GGA] | a (nm) [HSE] | Eg (eV) [GGA] | Eg (eV) [HSE] | Eg diff (eV)
BaTiO3 | 0.4038 | 0.3993 | 1.54 | 3.18 | 1.64
BaZrO3 | 0.4251 | 0.4228 | 2.99 | 4.51 | 1.51
CaTiO3 | 0.3896 | 0.3851 | 1.70 | 3.41 | 1.71
GdAlO3 | 0.3726 | 0.3684 | 2.90 | 4.33 | 1.43
GdGaO3 | 0.3843 | 0.3796 | 2.81 | 4.23 | 1.42
LaAlO3 | 0.3810 | 0.3777 | 3.49 | 4.89 | 1.39
LaGaO3 | 0.3928 | 0.3874 | 3.34 | 4.75 | 1.41
MgTiO3 | 0.3851 | 0.3800 | 1.60 | 3.18 | 1.58
ScAlO3 | 0.3646 | 0.3606 | 1.42 | 2.86 | 1.44
SrTiO3 | 0.3948 | 0.3905 | 1.65 | 3.33 | 1.69
SrZrO3 | 0.4194 | 0.4142 | 3.18 | 4.88 | 1.70
YAlO3 | 0.3718 | 0.3681 | 2.80 | 4.36 | 1.56

## Slide 9: Results VI
Electrostatic Potential, V
Band Alignment Calculations;
  Gives a Valence Band Offset of 0.44 eV
Displacement, x
LaAlO3-SrTiO3

## Slide 10: Results VII
0.98 eV
0.57 eV
Eg = 3.33 eV
Eg = 4.88 eV
Conduction Band
Valence Band
SrZrO3
SrTiO3
The Valence Band Offset is given by
where VBMi is the Valance Band Maximum of material i, and is the Averaged Electrostatic Potential in the bulk region of an interface calculation.

## Slide 11: Summary and Conclusions
The electronic bandstructure of cubic perovskites were determined from first principles.
The valence bands of oxide perovskite are composed mostly of oxygen p-states.
The conduction bands are determined by the B-cation orbitals.
The use of hybrid functionals increase the band gaps by 1.54±0.16 eV.
Most of the band offsets are determined by the conduction bands.

## Slide 12: Acknowledgements
My supervisor Dr. Anderson Janotti and faculty advisor Prof. Chris Van de Walle
Daniel Steiauf, John Lyons, Cyrus Dreyer, Luke Gordon and all the other members of the Van de Walle Computational Materials Group.
The School of Physics, The University of Dublin, Trinity College and the SFI.

## Slide 13: Thank you!